## Slide 1: LPCVD (SNU)
Single-run dep & diced wafer
Uniform films across wafer
Thickness limit : 200nm
Backside deposition Unsuitable for transmissive MS
H (nm) | Imaging (493nm) | Raman (532nm)
45 | 2.0193+i 0.0000 | 2.0123+i 0.0000
105 | 2.0390+i 0.0000 | 2.0302+i 0.0000

## Slide 2: PECVD (KANC)
Different piece process for h (400˚C)
Consistently higher n and k than PECVD at 493, 532nm
n - k vary by process to process
H (nm) | Imaging (493nm) | Raman (532nm)
650 | 2.0535+i 0.0008 | 2.0394+i 0.0001
900 | 2.0861+i 0.0012 | 2.0693+i 0.0001
950 | 2.0498+i 0.0005 | 2.0356+i 0.0000

## Slide 3: PECVD (KANC)
Different dep T (400˚C, 300˚C)
Similar trend to previous 400 ˚C process Higher Si content at 400˚C
300 ˚C process will be used for MS fabrication
T (˚C) | Imaging (493nm) | Raman (532nm)
300 | 2.0008+i 0.0000 | 1.9914+i 0.0000
400 | 2.0571+i 0.0005 | 2.0428+i 0.0000

## Slide 4: Fabrication window (Freeform MS)
Minimum feature (80%) : 60 nm
Minimum pitch (80%) : 80 nm
Not a direct comparison due to SiN sidewall angle issue
2 m
500 nm

## Slide 5: Summary
SiN n-k : 2.0008+i 0.0000 (493nm) , 1.9914+i 0.0000 (532nm)
Substrate : 2.5 x2.5 mm Fused quartz 500
Minimum feature/pitch : 60/80 nm
Aspect ratio (feature/pitch) 1:10
Expected height : Over 800nm
Has the target phase map or the required optical performance already been defined?
What does "tolerance" refer to in each of the requested data?
Question